## Slide 1: PRESENTATION ON USE of FLYASH in CONSTRUCTION
By
Gopal Varshney C.E., CPWD
CPWD Day

## Slide 2: Certain Facts Reg Fly ash
Annual Generation(2020) - 226.13 MT
Anticipated generation (2030) – 900 MT
Utilization - 187.81 MT (83%)
Area occupied (2020)- 65000 Acre
Major Areas of Utilization in construction industry:
  Cement – 25%
  Bricks & Tiles – 9.46%
  Road / Embankment/ Ash Dyke – 19.08%
  Reclaiming low lying area – 15.5%

## Slide 3: Certain Facts Reg Fly ash
Cost per 50 kg bag- Rs. 85/ Rs240 of OPC
Thermal power plant (Coal + Lignite) account for 54.7 % of total power generation
GST on fly ash product - 5%
Mobile app for availability of fly ash – ASHTRACK

## Slide 4: Production process

## Slide 5: Pollution cycle of fly ash

## Slide 6: Environmental consideration of disposal
Fly ash can casus all three environmental risks
Air : Direct emission of toxic chemicals from power plant and wind blown ash dust from mounds
Water : Wet system of disposal from power plant directly into near by surface water system
Ground : Long storage of ash can contaminate under line soil and under ground water

## Slide 7: Constituents of fly ash
Silica – Si O2
Lime – Ca O
Iron – Fe2 O3
Alumina – Al2 O3
And certain toxic chemicals

## Slide 8: Production v/s Utilization

## Slide 9: Major Modes of Fly Ash Utilization

## Slide 10: Percentage of fly ash used in:
PPC 35 %
Concrete Mix 35 %
Bricks 25 %
AAC block 65%

## Slide 11: Fly ash notification- A timeline
1991
Utilized 100% ash in 9 years (by 2009)
Mandatory use by construction agency within 50 km
2003
Radius increased from 50 km to 100 km
2009
Timeline revised for 100% utilization by 2014

## Slide 12: Fly ash notification- A timeline
2016
Radius increased from 100 to 300 km
Cost to be borne by thermal plant within 100 km
Equal share from 100 km to 300 km
Timeline extended to 2017
2020 (Draft)
Focus on pollutants rather than construction agencies
100% utilization within next 3 years
In case of none compliance provide fly ash free of cost to construction agency within 300 km and fine of Rs. 1000 per ton

## Slide 13
Filling in Road embankment
Filling in plinths of buildings
Fly-ash/FALG bricks
AAC block
PPC
Concrete Mixes
Concrete blocks
Paver blocks
In Base Course in Roads
Use of Fly Ash in construction industry

## Slide 14: Advantages of Fly ash
Environment friendly
Highly economical
Fine particles leads to less permeability
More resistance to acid and sulphate attack
Less Shrinkage
Good workability, durability and finish
Less generation of heat of hydration

## Slide 15: Disadvantage of Fly Ash
Poor control can lead to
Bad quality
Strength
Increase in permeability
Slower strength gain
(So more advantages than disadvantages)

## Slide 16: Fly Ash/Pond Ash
FLY ASH
  Fine particles carried along with gases collected by using electrostatic precipitator
  Has pozzolanic / silicious properties
  Used in replacing cement
POND ASH
  Collected in furnace bottom
  Embankment filling

## Slide 17
Project sanctioned in 2014 for Rs. 1200 crores with plinth area of 232000 sqm
Fly ash bricks, AAC Block, PPC and filling in road embankment
Case study – IIT Ropar

## Slide 18
Provision not kept in plinth filling due to fear of sulphate attack on concrete
But huge quantity required due to plinth level of 2 meters, forced reconsideration
Good earth rate – Rs. 400 per cum whereas fly ash for free was available in Ropar Thermal Plant 10 km away from site
The quality of fly ash got tested
The sulphate content found less then the required as per IRC:SP:58-2001
Case study – IIT Ropar

## Slide 19
S. no. | Parameters | Range as per IRC 58 | Results of sample
1 | Specific Gravity | 1.90-2.55 | 2.26
2 | Plasticity | Non-plastic | Non-plastic
3 | Maximum Dry Density (gm/cc) | 0.9-1.6 | 1.11
4 | Optimum Moisture Content (%) | 38.0-18.0 | 32.80
5 | Cohesion (kN/sqm) | Negligible | Nil
6 | Angle of Internal Friction (degree) | 30 – 40 | 34.9
7 | Coefficient of Consolidation (cm/ sec) | 1.75x10-5-2.01x10-5 | 1.24x10-4
8 | Compression index | 0.05-0.4 | 0.064
Case study – IIT Ropar

## Slide 20
S. no. | Parameters | Range as per IRC 58 | Results of sample
9 | Permeability (cm/sec) | 8x10-6-7x10-4 | 5.14x10-5
10 | Particle size distribution (% of materials) |  | 
 | Clay size fraction | 1-10 | 4.8
 | Silt size fraction | 8-85 | 78.4
 | Sand size fraction | 7-90 | 16.8
 | Gravel size fraction | 0-10 | 0
11 | Coefficient of Uniformity | 3.1-10.7 | 7.74
12 | Soluble Sulphate content (gm/litre) | 1.9 | 0.02
Case study – IIT Ropar

## Slide 21: Case study – IIT Ropar
Columns casted till bottom of the plinth beam
Filling with pond ash
Three layers of compacted 15 cm depth of pond ash (Dry density 95 %)
Intermediatory layer of 15 cm earth (Soil density 98%)
Top and side layer of 30 cm earth

## Slide 22: Case study – IIT Ropar

## Slide 23
Case study – IIT Ropar
Stacking of pond ash at site

## Slide 24
Case study – IIT Ropar
Compaction of layers by roller

## Slide 25
Case study – IIT Ropar
Compaction of layers by roller

## Slide 26
Case study – IIT Ropar
Compaction of layers by roller

## Slide 27
Case study – IIT Ropar
Compacted layers

## Slide 28
Case study – IIT Ropar
Filling of earth and pond ash in layers

## Slide 29
Case study – IIT Ropar
Compaction within plinth with earth compactor

## Slide 30: Checking density of fly ash

## Slide 31: Filling in plinth

## Slide 32: Fly ash in embankment

## Slide 33: Fly ash in embankment

## Slide 34: Use in CAPFIMS till now
Fly ash brick – 2,071 MT
AAC block – 2,227 MT
Fly in concrete mix 25,196 MT
PPC – 3,586 MT

## Slide 35: References for usage of fly ash in construction
Road embankment – IRC SP:58-2001
C/o rural roads – IRC SP:20-2003
For use in cement mortar / concrete – IS:3812-2003
Fly ash bricks – IS:12894, IS:16720, IS:13757
For use in base course in roads - IRC:60

## Slide 37
THANK YOU