## Slide 1: Flexible Pavements Solutions
Dr. Ratnakar R. Mahajan
Deputy General Manager
Maccaferri Environmental Solutions Pvt. Ltd.

## Slide 2: Content
Flexible Pavement
Flexible Pavement – Failure Mode
Asphalt Reinforcement
Geosynthetic Solution
Drainage
Case Studies

## Slide 3
FLEXIBLE
PAVEMENT &
FAILURE MODE

## Slide 4
Main structural element (durable)
BOUND MATERIAL
Pavement foundation
GRANULAR MATERIALS
BOUND MATERIAL: high stiffness, crack and deformation resistant
GRANULAR MATERIAL OVER SOIL: adequate platform to place layers above
WEARING COURSE
BINDER
BITUMINOUS BASE
BASE
SUBBASE (optional)
SUBGRADE
Pavements: Terminology
Existing soil
Notes: 2

## Slide 5
Surface cracking is the most visible sign of pavement deterioration
Once cracking occurs, surface water can penetrate to the underlying road construction. This in-turn can cause the premature failure of the entire pavement.
The mechanisms of failure may be categorized as
Reflective cracking
Traffic induced
Thermally induced
Surface initiated
Flexible Pavement Failure

## Slide 6
Fatigue cracking
Rutting, Shoving/ structural
Longitudinal / settlement
Edge break/ haunching
Flexible Pavement Failure

## Slide 7: Failures in Flexible Pavements
Different types of failure encountered in flexible pavements are as follow.
Fatigue cracking
Rutting
Longitudinal cracking
Transverse Cracking
Pot Holes
Slippage cracking

## Slide 8
GEOSYNTHETIC
SOLUTION

## Slide 9
Geosynthetics for pavements

## Slide 10: Geosynthetics for pavements
SEPARATION: to prevent the intrusion of fines from the subgrade into the base layer due to traffic loads
FILTERING: to prevent fine particles being washed from the subgrade into the base layer due to water
REINFORCEMENT: to improve the tensile strength of a pavement layer
MOISTURE BARRIER: to abate water infiltration to the underneath pavement layers
STRESS RELIEF: to allow for larger deformations in the interlayer by dissipating the energy
6. Drainage: to enhance the drainage of graded aggregate layers

## Slide 11
RoadMesh / Paving Fabric / Glassgrid: Reinforcement of surface course (asphalt layer) / bearing course
Biaxial Extruded geogrid / Woven Geogrid : reinforcement of granular layer (i.e. Base course and Sub-base course)
Drainage Composite : For drainage and / or filter/separator
GLASSGRID/ROADMESH
Extruded /Woven Geogrid
Drainage Composite
Geosynthetics For Pavements

## Slide 12
ASPHALT REINFORCEMENT
When a geosynthetic is placed as a tensile element within the BOUND layer, to increase the service life of the pavement by preventing fatigue and reflective cracks
BASE AND SUBBASE STABILISATION
When a geosynthetic is placed as a tensile element at the bottom or within a flexible UNBOUND base (or sub-base) course to eventually increase resilient modulus of unbound layer & bearing capacity of the subgrade thus having:
(i) improvement of the service life;
(ii) an equivalent performance with a reduced structural section;
BASAL REINFORCEMENT
The reinforcement is used at the embankment-subgrade interface to enhance the resistance of the embankment to avoid failure through excessive deformation or shear in the foundation
Geogrids in Pavement

## Slide 13
ASPHALT REINFORCEMENT
SOIL STABILISATION
BASAL REINFORCEMENT
Unbound layers
Bound layers

## Slide 14
BASE and SUBASE
STABILIZATION

## Slide 15
WITHOUT BASE STABILIZATION
WITH BASE STABILIZATION
Geogrid
Base and Subbase Stabilization

## Slide 16
Geogrids are widely used in developed countries in pavement structures to improve performance or reduce thickness of pavement.
Geogrids in Pavement

## Slide 17: Solution Components
Extruded Geogrid i.e. MacGrid EG
Extruded geogrids are polypropylene geogrids produced by an extrusion process characterized by a tensile resistance both in the longitudinal and cross direction
It exhibits high modulus and high strength at low elongations providing tensile reinforcement to soil and aggregate structures

## Slide 18: Solution Components
Extruded Geogrid i.e. MacGrid EG
The high tensile strength and junction efficiency of biaxial geogrids
confines and restrains aggregate from lateral movement, ensuring proper
distribution of imposed stresses and ultimately extending the service life

## Slide 19
Reinforcing the Base and Subbase With Geogrid
3- tensioned membrane effect;
4- separation effect (GT)
Mechanism
1- lateral confinement;
2- load distribution;

## Slide 20
Thickness reduction at equal values of c, φ, N;
Base course reduction (BCR)
percent reduction in the reinforced base, or subbase thickness from the unreinforced thickness, with the same material constituents, to reach the same defined failure state
Benefits of Base and Subbase stabilization

## Slide 21
Lifetime increase at equal values of h, c, φ;
Traffic benefit ratio (TBR)
ratio of the number of load cycles on reinforced section to the number of load cycles on an unreinforced section, with same geometry and material constituents, to reach the same defined failure state.
TBR is sometimes termed
traffic improvement factor (TIF)
Benefits of base and subbase stabilization

## Slide 22
Reduce the quality of fill at equal values of N, h
Reduces the requirement for good quality
virgin unbound aggregate
Geogrid improves the mechanical properties
i.e modulus and bearing capacity of local low quality/marginal aggregates
Benefits of base and subbase stabilisation

## Slide 23
Reinforced Section of Pavement
W.C.
BINDER
BASE
SUBBASE
SUBGRADE
Geogrid
Design Methodology of Geogrid Reinforced Pavement
Geogrid

## Slide 24
Despite many successful projects and research it is recognized that the use of geogrid reinforcement in paved roadways is relatively limited compared to other geosynthetics applications.
Major reasons for limited used of geogrids in base reinforcement applications
Geogrids (and geosynthetics in general) are perceived as special materials that are considered only if problem areas need to be fixed (Gabr et al., 2006).
Existing numerical models for pavement design without geosynthetics are complicated and perception is that inclusion of geosynthetics will complicate further.
Ref. Berg et al. (2000), Perkins et al. (2005c), and Gabr et al. (2006)
Design Methodology of Geogrid Reinforced Pavement

## Slide 25
Empirical
Limiting shear failure
Limiting deflection
Regression methods,
Mechanistic-Empirical
Existing design methods-AASHTO 1993
W18 = predicted number of 80 kN (18 kips) ESALs
ZR = standard normal deviate (example: ZR = -1.645 for 95 % reliability)
So = combined standard error of the traffic prediction and performance
prediction
SN = Structural Number (an index that is indicative of the
total pavement thickness required) [inches]
= a1D1 + a2D2m2 + a3D3m3+...
ai = ith layer coefficient
Di = ith layer thickness (inches)
mi = ith layer drainage coefficient
ΔPSI = difference between the initial design serviceability index, Po, and the
design terminal serviceability index, Pt
MR = Subgrade resilient modulus (in psi)

## Slide 26
26
AASHTO method for reinforced roads
The structural contribution of a geogrid can be quantified by the increase in the layer coefficient of the aggregate base and subbase course.
SN Equation now becomes:
SN = a1d1 + LCR1 a2d2M2 + LCR2 a3d3M3
Where:
LCR = Layer Coefficient Ratio
SN: Structural Number
a1, a2, a3,... – ith layer coefficient
d1, d2, d3.... –ith layer thickness
M2, M3....-ith layer drainage coefficient
Design Methodology of Geogrid Reinforced Pavement

## Slide 27
27
Complexity of layered pavement system and loading conditions- simple design method for incorporating Geogrid reinforcement
Series of performance tests to evaluate contribution of geogrid to derive design parameters & incorporating into a design methodology.
Early design approaches to be modified to reflect the benefit achieved by the addition of geogrid by a pavement reinforcement design term Viz., LCR.
LCR — Layer Coefficient Ratio: A modifier applied to the layer coefficient of the aggregate.
Geogrid reinforced pavements
How to incorporate Geogrid properties in Pavement
W.C.
BINDER
BASE
SUBBASE
SUBGRADE
Geogrid
Geogrid

## Slide 28
CRITICAL PARAMETERS FOR PAVEMENT DESIGN
Tensile strain, Єt, at the bottom of the bituminous layer and
The vertical subgrade strain, Єv, on the top of the subgrade
to limit cracking and rutting in the bituminous layers and non-bituminous layers respectively.
Design method - IRC 37 (2012)

## Slide 29
Fatigue Model (Bottom up cracking)
Nf = 2.21 * 10-04 x [1/εt]3.89 * [1/MR]0.854
(80 per cent reliability)
Nf = 0.711 * 10-04 x [1/εt]3.89 * [1/MR]0.854
(90 per cent reliability)
Where,
Nf = fatigue life in number of standard axles,
εt = Maximum Tensile strain at the bottom of the bituminous layer, and
MR = resilient modulus of the bituminous layer.
Rutting model
N = 4.1656 x 10-08 [1/εv] 4.5337
(80 per cent reliability)
N = 1.41x 10-8x [1/εv] 4.5337
(90 per cent reliability)
Where,
N = Number of cumulative standard axles, and
εv = Vertical strain in the subgrade
Design method - IRC 37 (2012)

## Slide 30
Design example
Design Considerations
Design Traffic load – 150msa
Reliability Factor - 90%
Design life – 20 years
Design Subgrade CBR 3%
PSI- 1.7
Drainage Coefficients m2=m3=1
Unreinforced Section as per IRC 37 & AASHTO 1993

## Slide 31
Considering Maccaferri extruded geogrids MacGrid EG40S in both base and subbase. LCR for base and subbase are 1.40 and 1.73 respectively
Design example
Reinforced layer coefficients and Corresponding Elastic modulus

## Slide 32
By using modified layer coefficients in eqn SN we get Reinforced section thickness
By putting the above obtained thickness,In IITPAVE with improved Elastic modulus values,
we get NF and NR to determine the fatigue and rutting resistance of reinforced pavement.
Maximum tensile strain at bottom of surface layer= 86 micro strains
Corresponding NF= 180 MSA >150MSA
Maximum compressive strain at top of subgrade = 291 micro strains
Corresponding NR = 209 MSA >150MSA
Design example

## Slide 33: Another Example
Pavement Layer | IRC 37 | Rates | Modified AASTHO |  | 
 | Unreinforced | Per cum | Reinforced in Base | Reinforced in Sub-base | Reinforced in both layers
BC (mm) | 50 | 10370 | 50 | 50 | 50
DBM (mm) | 155 | 9950 | 155 | 155 | 155
GB (mm) | 250 | 3500 | 180 | 250 | 180
GSB (mm) | 380 | 3000 | 380 | 220 | 220
Total Thickness (mm) | 835 |  | 765 | 675 | 605
% reduction in thickness |  |  | 8% | 19% | 27.5%
Cost per linear meter | 4075 |  | 3980 | 3745 | 3650
% saving |  |  | 2.3 | 8.1 | 10.4
Saving per km (Lakh) |  |  | 1 | 3.3 | 4.25
Saving for 100 km project |  |  | 1 Cr | 3.3Cr | 4.25 Cr
Designed pavement section thickness Subgrade CBR is 3% and number of traffic passes during the design life of the pavement is 100 msa. Reinforcement MacGrid EG 40S

## Slide 34
Indicated numbers are showing direct cost saving.
Indirect saving (Tangible and Non Tangible)
Reduced section require lesser material which means lower transportation cost.
Less material means faster construction compared to conventional pavement.
Less movement of construction equipment means lower maintenance cost which nobody think.
Lower movement of dumper, compactor, mixers and other equipment directly result in lower carbon emission. Environment Friendly solution.

## Slide 35
HOW DO I DESIGN
PAVEMENT? DO YOU
HAVE SOFTWARE?

## Slide 37
MACREAD 2.0 Software Output

## Slide 38: CODAL STANDARDS AND RFERENCES
Notes: To ensure the quality and the products are inaccordance with the codal standards

## Slide 39
It is good solution however
My project do not have aggregates or materials as per IRC & MORTH specifications. How can geosynthetic work in this situation?
Locally available material
?

## Slide 40
Geogrid Reinforced Pavement : Field Trial Stretch Testing
For both section i.e. for reinforced and unreinforced section, the testing has been performed
The following field test has been conducted,
Field CBR test
Cyclic plate load test
Plate Load test
Field Density test

## Slide 41: Section Components
Geogrid : Two layers of biaxial geogrid i.e. Macgrid EG one over the subgrade

## Slide 42
Subgrade: Natural subgrade was reasonably uniform across the site and the same has been leveled and compacted for the trial stretch.
Section Components

## Slide 43
Subbase course
Locally available material from the river Dimdima is soil chosen as the subbase course material. The source is approximately 50km from the either ends of the project corridor.
Locally available material is the low cost material available with minimum required properties and in required quantity sufficient for the whole stretch construction.
Section Components

## Slide 44
Subbase Course Soil Gradation
Chart: Particle Size (mm)
| 80 | 53 | 45 | 22.4 | 11.2 | 4.75 | 2.36 | 0.6 | 7.4999999999999997E-2
Subbase Gradaion | 100 | 100 | 100 | 91.2625 | 77.625 | 57.2 | 52.6875 | 30 | 5.225

## Slide 45: Trial Stretch Construction & Testing
Cleared, grubbed and leveled the shoulder portion
Compacted the subgrade uniformly to minimum 95% MDD at OMC
After Subgrade formation, the CBR, Density and Moisture content test has been performed
Photograph of Compacted Subgrade

## Slide 46: Trial Stretch Construction & Testing
Photograph of Securing Geogrid with steel U pins
Photograph during Laying of Geogrid on the prepared subgrade
On the prepared subgrade of reinforced section, MacGrid EG 30S of required length has been installed at the required level as per the design sections
As per the Installation guideline MacGrid EG has been laid over the subgrade

## Slide 47: Trial Stretch Construction & Testing
Laid the subbase course soil in uniform layers with grader on prepared surface and compacted each layer not more than of 150 mm thickness with smooth wheel roller.
On prepared subbase layer the CBR, density and moisture content test has been performed
Photograph of Laying, Spreading using grader for preparation of Subbase

## Slide 48
Field Density:
Field density has been performed by using sand replacement method as per the code IS IS 2720-28 (1974): Methods of test for soils, Part 28: Determination of dry density of soils in-place, by the sand replacement method.
Field density has been checked for every compacted layer for ensuring the compaction of minimum 95% MDD
Minimum three tests were performed at different locations on the prepared surface

## Slide 49: Field CBR Test
Field CBR was performed as per IS 2720 (Part 31): 1990: Methods of tests for soils, part 31, Field determination of California Bearing Ratio.
Field CBR test is performed on the prepared subgrade and subbase for both reinforced and unreinforced Sections
Minimum three CBR tests were conducted on prepared surfaces
Field Tests Performed

## Slide 50
Plate Load test
Plate load test was performed as per IS 9214 (1979): Method of determination of modulus of subgrade reaction (K-Value) of soils in field
Plate load test has been performed on the prepared subgrade and subbase of both reinforced and unreinforced sections
On each layer minimum one plate load test has been performed to understand the modulus of soil reaction of the respective layer.
In this trial test , square plate of 30cm X 30cm size has been used
Field Tests Performed

## Slide 51
Cyclic Plate load test:
Cyclic plate load test was performed as per IS 5249 (1992): Determination of dynamic properties of soil - Method of test
Cyclic plate load test was performed on the prepared subgrade and subbase of both reinforced and unreinforced sections.
On each layer minimum one cyclic plate load test was conducted for understanding the settlements corresponding to no. of cycles repeated for reinforced and unreinforced sections.
Field Tests Performed

## Slide 52: Summary of Test Results
Field Density Test
Field density and moisture content on each compacted layer has been tested and the average density and moisture content are as shown in the table below.

## Slide 53
Summary of Test Results
Field California Bearing Ratio Test Results (CBR Test Results)
Above table clearly indicates that CBR of reinforced section is higher than unreinforced section.
Improvement of 78.7% in CBR is observed for reinforced section which confirms the positive benefit of using extruded biaxial geogrid in the pavement section

## Slide 54: Summary of Test Results
CBR and soil modulus E (in MPA) are linked by the relationship used in AASHTO 1993 guidelines:
Mr = 17.6 (CBR)0.64 (MPa)
Hence we get the following values
Modulus improvement of subbase is 45%
Above table clearly shows Geogrids shall increase the E of base and subbase.

## Slide 55
In AASHTO 1993 guidelines the layer coefficient a3 of subbase are linked to the modulus ESB subbase by the following relationships
a3 = 0.227 log10 (145 Esb) – 0.839 (Page II-22)
layer coefficients a3 (for unreinforced conditions) and a3’ (for reinforced conditions) from above equations are
Hence this very simple field test, even without any traffic applied, confirms that geogrids are able to increase the layer coefficients of base and subbase.
Summary of Test Results

## Slide 56
Percentage improvement of Subbase soil reaction modulus K is 11%

## Slide 57
Summary of test Results-
Cyclic Plate load test
Cyclic plate load test on Subbase course
Above graph of subbase indicates the lower settlements for unreinforced section for initial 6 repetitions and for further repetitions reinforced section has lower settlements than unreinforced section and this decrement of settlement increases with increase in number of cycles

## Slide 58: Locally Available Material can used
With this solution savings can be more e.g. 20% or more
Most important progress of the project is not hampered
Environment Friendly Solution

## Slide 59
ASPHALT
REINFORCEMENT

## Slide 60
Asphalt Reinforcement
Reinforcement provides a lateral restraint within the asphalt that produces a threefold increase in the service life of pavements by relieving and redistributing stress concentrations

## Slide 61
COMPRESSION
STRESS DISTRIBUTION
ASPHALT LAYERS
SUBBASE
TENSION
SUBGRADE
Without Asphalt Reinforcement
Notes: 61
The stress distribution of a (flexible) pavement looks in general like shown in this picture. High tensile stresses at the lower part of the bituminuous surface cause cracks which easily and rapidly grow through the upper part to the surface.

## Slide 62
COMPRESSION
STRESS DISTRIBUTION
ASPHALT LAYERS
SUBBASE
TENSION
SUBGRADE
Tension taken by reinforcement
With Asphalt Reinforcement
Notes: 62
Mesh Track inhibits the initiation of cracks at the bottom of the asphalt layer by absorption of the tensile stresses by the Steel Mesh. As a consequence, the bituminuous products are no longer subject to tension and will not crack by bottom-up fatigue.

## Slide 63
MacGrid AR G – Glass fibre woven geogrid
Roadmesh – Wire mesh
Asphalt Reinforcement

## Slide 64
Glass grid ( Macgrid AR G) is a glass fiber geogrid with coating.
With high tensile strength and high modulus of elasticity at low elongation
designed to control reflective cracking.
Glass grids can be with geotextile backing, impregnated with bitumen to
provide crack prevention with a waterproof membrane and improved bond
between the asphalt layers.
Asphalt Reinforcement

## Slide 65
Road Mesh : Unique Properties
Bi Directional Strength
Full Interlock Into Matrix
3D Open Structure
  Stands clear of surface - “W” profile
  Allows compaction around the wire strands
Robust
Asphalt Reinforcement
Notes: 65
So Product has Bi Directional Strength to resist the BiDirectional Loading which occurs in a pavement.
Unique Geometry allows mesh to Interlock with Aggregate, so if you core, you only see a cross section of a single strand of wire - Acting like a Piece of Agg
The 3D open structure allows the Asphalt to Lie in the Voids and Bond to the Underlying Layer.
The Product is also Able to Withstand Construction Traffic during Installation.

## Slide 66
66
GS in the bound layers
For MacGrid AR and ROAD MESH it is possible to design:
A) reinforced overlays by means of OLCRACK software (Prof. Brown, Nottingham University)
B) pavement rehabilitation (for Road Mesh only) by means of a design equation (Prof. Al-Qadi, USA)
Paved roads: reinforcement of the bound layers

## Slide 67
Overlay

## Slide 68
Road Widening Solution
When roads need to be widened, differential settlement cracks occur at the junction between the old and new pavement structures.
Road Mesh is introduced to bridge the junction to absorb the crack stresses caused by the differential settlement.
The effective interlock with the asphalt aggregate matrix ensures the optimum contribution of the Road Mesh.
Applications of Road Mesh

## Slide 69
69
Log Wt80 = aHoverlay + bEoverlay + cHHMA + dEHMA + eHbase + fEbase + gEsubgrade
Where:
a, b, c, d, e, f, g = regression constants
Wt80 = total number of 80-kN single-axle load applications;
Hoverlay = thickness of HMA overlay (mm);
Eoverlay = modulus of resilience of HMA overlay (MPa);
HHMA = thickness of existing HMA layer (mm);
EHMA = modulus of resilience of existing HMA layer (MPa);
Hbase = thickness of base layer (mm);
Ebase = modulus of resilience of base layer (MPa);
Esubgrade = modulus of resilience of subgrade (MPa).
ROADMESH IN OVERLAYS: Al-Qadi’s Equation
Paved roads: reinforcement of the bound layers

## Slide 70: Paved roads: reinforcement of the bound layers
Maccaferri’s pavement products have been developed through an extensive program of international research.
Smart Road, Virginia Tech, USA
Full scale instrumented field trials showed Road Mesh produced a 72% decrease in strain and a fatigue life improvement of up to 120%.
Nottingham University, UK
Beam bending tests showed Road Mesh can reduce thermal cracking and extend the service life of asphalt overlays by three times. Wheel track tests showed Road Mesh can half the depth of rutting.
SMES, Italy
Cyclic loading showed Road Mesh can extend the service life of asphalt pavements by three times.
13°C
Road Mesh
Control
12kN Repetitions
Deformation [mm]
Road Mesh
20°C
Control
SUMMARY OF RUT RESULTS

## Slide 71
71
ROADMESH IN OVERLAYS: OLCRACK software
Paved roads: reinforcement of the bound layers

## Slide 72
72
ROADMESH IN OVERLAYS:
OLCRACK software
Paved roads: reinforcement of the bound layers

## Slide 73
The Road mesh is preferred for Asphalt Reinforcement due to its unique geometry and 3D structure that allows full compaction to occur around the wire strands resulting in full interlock with the asphalt matrix.
It’s double twist avoids spreading of the damage caused by the accidental breaking of any wire or mesh.
Road Mesh also extends life of pavement
Road mesh is able to withstand construction traffic
Road Mesh is preferred for Reinforcement of surface course as asphalt reinforcement

## Slide 74
Changes crack behaviour in asphalt
  Delayed initiation
  Slower growth
  Narrower width
  Wider spacing
  Deviation at grid
Lateral restraint
  Reduces rutting and shoving
  Little effect on modulus in the short term
  Cost benefit up to 35%
Overlays
  Extends life x 1.4 – 1.9
  Most benefit for thicker overlays (> 75mm)
Benefits of Asphalt reinforcement

## Slide 75
DRAINAGE

## Slide 76: Drainage- Conventional approach
Traditionally, gravel layer is provided as the draining layer
Provision of graded aggregates in the subbase course in order to effectively drain the water from the pavement structure
Provision of french drains (Trench with free drain materials)
Functions of French drains are
    Collect surface water run-off
    Control ground water flow
    Lower the high ground water table

## Slide 77: Problems associated with conventional approach
Satisfying the drainage criterion for conventional graded filter design is extremely expensive.- Non availability of required aggregates
Clogging: Ground water flows towards the drain carrying some fine particles from the base soil and consequently, the aggregates become blocked after some period having no adequate water removal capacity.
Internal erosion of the base soil
Requires considerable time for installation as it is to be installed as per gradation
Require Skilled labor
Material quantity and quality tend to differ along the length of the wall due to construction sourcing and human error issues.
Increase in carbon footprints and Pressure on natural resources

## Slide 78: Alternatives?
Geosynthetics
Drainage solutions using Geocomposite Drainage

## Slide 79
Drainage geocomposites are composed of a geotextile filter surrounding either a geonet (blanket drain), a thick preformed core (panel or edge drain), or a thin preformed core (wick drain). Some applications of drainage geocomposite are blanket drains and edge drains.
Drainage Geocomposite - MacDrain

## Slide 80
Principles of the functions afforded by Drainage geocomposite
Drainage geocomposite- MacDrain

## Slide 81
Road Side Drain Edge Drain: using Drainage Composite
Drainage of Structures
Drainage Geocomposite - MacDrain

## Slide 82
Geocomposite To Replace Subsurface Drainage Layer For Pavements

## Slide 83
Solutions with MacDrain
Sub-Surface Drainage
- Sub-Superficial Drainage
- MacDrain Drainage

## Slide 84: Conventional Solution
Filter behind retaining wall
GSB – granular layer in pavement

## Slide 85
MORTH 700

## Slide 86
Trench and Edge Drains
Drainage Geocomposite - MacDrain

## Slide 87
CASE STUDIES

## Slide 88: Creek kalatalav sanesh road, Bhavnagar, Gujarat
Previous Site Conditions
Poor Soil properties
Low CBR value, soft soil
Critical site conditions i.e possibilities of the Water on both sides of the road
Heavy loading (Salt Industries and Sheep breaking industries nearby)

## Slide 89
Creek kalatalav sanesh road, Bhavnagar, Gujarat,,

## Slide 90
  Solution:
    High Strength Unidirectional Geogrid (ParaLink) having tensile strength 200 kN/m as basal reinforcement to improve the subgrade properties
    Geotextile (MacTex) was used as separator
    Extruded polypropylene biaxial geogrid (MacGrid EG) of strength 40 kN/m as reinforcing material
    Drainage composite (MacDrain) was used in edge drains to drain out the surface runoff
    Double twist mesh with longitudinal shooting bars (Road Mesh) was provided which can effectively prevent fatigue cracking, surface rutting etc.
Creek kalatalav sanesh road, Bhavnagar, Gujarat

## Slide 91
Creek kalatalav sanesh road, Bhavnagar, Gujarat

## Slide 92: Inference from this case study
Paved roads can be constructed on soft soil have very low CBR
On soft subgrade pavement with lower thickness can be built.
Road widening problem can be dealt using geosynthetics

## Slide 93: Problem:
Nadia-Kapadwanj- Modasa road stretch was subjected to severe problem of series of interconnected cracks.
Due to the increased traffic, the existing pavement section was not able to survive for its initial design life.
Existing pavement had cracks developed on the surface which had deteriorated further into large potholes.
Considering the pavement situations and heavy traffic loading it was required to re-strengthen the pavement by providing an overlay of suitable thickness.
Pavement Strengthening at Nadia - Kapadwanj - Modasa Road

## Slide 94
Current pavement was needed to be repaired by placing an asphalt layer to increase the load carrying capacity of the pavement section.
However the ability of asphalt to withstand tensile stress is limited. So there were chances of fatigue and reflective cracking in the surface course.
To avoid this type of cracking, Geosynthetic reinforcement are introduced between new overlay and the existing pavement.
For reinforcing pavement, Geogrid made of fiber glass yarns called as MacGrid AR V5 was suggested to be provided at the interface of the BUSG and BM layer.
For ensuring proper adhesion of the MacGrid to the surface, tack coat is applied over the BUSG layer before laying the MacGrid.
MacGrid AR V is a reinforcing material specially developed for pavements. It consists of glass fibre strands arranged in a grid structure and covered with a polymer coating.
Pavement Strengthening at Nadia - Kapadwanj - Modasa Road

## Slide 95
Pavement Strengthening at Nadia - Kapadwanj - Modasa Road

## Slide 96
ROADMESH
Road Mesh installation was done in the year 2000, on the
pilot scale, for Pavement Stabilization at Ambala, Punjab.

## Slide 97: Construction of Unpaved Road, Haldia, West Bengal,

## Slide 98: Construction of Unpaved Road, Haldia, West Bengal,
Unrolling Geotextile (MacTex)
Laying brickbat and aggregate over geogrid
(MacGrid)
Sand Filling
Laying MacGrid WG4S
Completed Road
Completed Road after one year
Present Status of the Project The Project was successfully completed in 2010 and working successfully for intended purpose.

## Slide 99: Existing masonry retaining wall Placing of the MacDrain
Six Laning Of Gurgaon-kotputli-jaipur Section Of Nh-8

## Slide 100: Seepage from the weep holes MacDrain checked after the test

## Slide 101: Four laning of Hyderabad –Karimnagar-Ramakundam Road
The backfill material used was fly ash.
As per MORTH requirement, 600 mm thick graded gravel filter is provided behind the panels.
This 600 mm thick gravel graded filter is replaced with MacDrain as shown in the figure.

## Slide 102
Installed MacDrain and simultaneous backfilling process

## Slide 103
RECAP
RE-CAP…

## Slide 104: Recap
ASPHALT REINFORCEMENT
Applicable new roads
Resurfacing of roads
RoadMesh & Glassgrid (Better performance)
BASE AND SUBBASE STABILISATION
Applicable new roads
Repair of road which include base or subbase stabilization
Use of locally available materail
DRAINAGE
Edge Drains
Capillary Cut off

## Slide 105: Summary
Use of Geosynthetics in pavements provides following benefits:
Separation/Filtration layer
Reduce vertical and lateral deformation
Increase the bearing capacity of soft soil
Allows the use of Marginal/ Recycled/ locally available materials effectively
Better drainage
Extended Serviceability of the road i.e. Traffic benefit Ratio (TBR)
Reduction in Crust thickness i.e. Base Course Reduction ( BCR)
Less periodical maintenance
Reduce construction and operational costs
Lower Carbon Footprint

## Slide 106
THANK YOU
Questions are Welcome
Please contact us on
info@maccaferri-india.com
info@in.maccaferri.com
Dr. Ratnakar R. Mahajan
Deputy General Manager
Maccaferri Environmental Solutions Pvt. Ltd.
Mob:+91-9987050096
ratnwdc@maccaferri-india.com