## Slide 1
CLIMATE RESISTANT SAFER HILL ROADS
“MY COUNTRY WAS NEVER SO RICH THAT IT COULD AFFORD POOR ROADS”

## Slide 2
BUILD SUSTAINABLE ASSETS
Notes: Nano level modification & treatment

## Slide 3
HILL ROADS: CRITICAL ISSUES
Expensive to transport materials so it is imperative to use in-situ / local materials
Inconsistent compaction due to cooler temperatures and wind speed
High Shear in Bitumen Layers on curves, extreme slopes and higher loads
Resistance to salt on bituminous layers
Rain cuts on the side slopes

## Slide 4
Stripping
Raveling & Pot Holes
365 DAY HEAVY CONDENSATION IN PAVEMENTS
Air Gaps
Water
Gets in
Water
Evaporates
& Expands
Potholes, raveling and undulations can lead to loss of vehicle grip and speed

## Slide 5
Fatigue Cracking & Rutting
Temperature Difference
EXPANSION & CONTRACTION CYCLES

## Slide 6
Undulations
Larger Cracks & Weakening of sub-grade soil
FREEZE-THAW CYCLES

## Slide 7
CRACKING DUE TO SUDDEN DROP IN TEMPERATURE

## Slide 8
BITUMEN DETERIORATION DUE TO UV RADIATION

## Slide 9
SAFETY
Potholes Elimination ?
Salt Effects Elimination ?
Rutting Elimination ?
Cracks Elimination ?

## Slide 10
Hill Roads – BETTER ROADS
ASPHALT LAYERS |  | 
CRITICAL FACTOR | NANOTECHNOLOGY | BENEFITS
Poor Compaction Bitumen Bonding to Aggregates | Nano modification of aggregates and ability to improve workability at very low temperature is the key | Consistent higher density at lower temperature Resistance to salt water

## Slide 11
PHYSICAL TO Chemical Bonding
Basalt Granite Limestone
Aggregate Surface with ZycoTherm Nano Layer
Weak Physical Bonding
Strong Chemical Bonding

## Slide 12
BOIL SALT TEST ASTM D3625 : EXTEND TO 6 HOURS
PG 64-22 / VG 30 / 60-70 Pen
PG 76-22
Chart: 
| PMB Control 165 C | PMB + 0.1% ZycoTherm 135 C
10 Min | 98 | 98
1 Hr | 65 | 98
6 Hr | 10 | 98
Chart: 
| Control 135 C | Control 120 C | 1% Hydrated Lime 135 C | 0.5% Amine 135 C | 0.1% ZycoTherm 120 C
10 Min | 59 | 15 | 65 | 60 | 95
1 Hr | 10 | 5 | 25 | 15 | 95
6 Hr | 5 | 2 | 10 | 5 | 85
Basalt Aggregate (DBM) : 45% 20 mm, 10% 10 mm, 45% less than 6 mm with stone dust
Asphalt Grade: AC-20 (VG-30, 60-70 penetration grade)

## Slide 13
WATER PENETRATION DEPTH UNDER PRESSURE : ASTM D 6927 : 2005A
Description | Control |  | ZycoTherm |  |  |  |  | 
Sample No. | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16
ZycoTherm % | 0 | 0 | 0.025 | 0.025 | 0.05 | 0.05 | 0.10 | 0.10
Maximum Penetration (mm) | 5 | 3 | 0 | 2 | 2 | 3 | 0 | 0

## Slide 14
Mix Type | Binder Type | C / ZT | Compaction Temp OC | 50 % Coating Sec | Compaction Resistance 21Nm | Void Content Vol %
AC 16 BS | 50/70 | C | 135 | 25 | 41.6 | 7.0
 |  | ZT | 135 | 15 | 43.5 | 7.1
 |  |  | 115 | 19 | 42.8 | 7.2
 |  |  | 95 | 19 | 41.3 | 6.9
AC 11 DS | 25/55-55 A | C | 145 | 37 | 37.3 | 4.3
 |  | ZT | 145 | 22 | 34.2 | 4.6
 |  |  | 125 | 30 | 36.5 | 5.0
 |  |  | 105 | 30 | 36.5 | 5.3
COMPACTION RESISTANCE at lower
TEMPERATURE
Innovationsgesellschaft Technische Universität Braunschweig mbH

## Slide 15
UPSHI SARCHU MOUNTAIN ROAD, LEH 2011
Laying Nano mix 2011
Control 2012
Nano Bonded layer 2015

## Slide 16
KUYUL PHOTILE CHISUMLE ZURSAR INDO CHINA ROAD @ 14000 FEET LAYING AT -10 C

## Slide 17
INDUSTRIAL ROAD
40 mm Wearing Course with VG 30; 3 kms 2 lanes
June 2016
April 2009

## Slide 18
SAFETY
Cracking due to the shear forces of tires turning on the curves will be eliminated
Chemical bonding and waterproofing will ensure pavement behaves as a monolithic composite giving better grip

## Slide 19
Hill Roads – BETTER ROADS
BOND COATS |  | 
CRITICAL FACTOR | NANOTECHNOLOGY | BENEFITS
100 % Coverage & Waterproofed surface with reduced tracking | Nano compounds promote bonding and make bond coats penetrative and waterproofed | Layers behave like an integrated waterproofed composite. High Shear on roads curves is taken care due to higher bond strength

## Slide 20
TACK COAT BOND STRENGTH
CSS1H (60%); Mix 2 emulsion diluted with water and added with Nanotac (Residual bitumen 30%)
Parameters | Mix # 1 Control Mix |  |  | Mix # 2 Test Mix |  | 
Specimen No. | C1 | C2 | C3 | T1 | T2 | T3
Failure Load kN | 3.25 | 3.40 | 3.15 | 4.85 | 5.8 | 5.35
Shear Stress | 0.41 | 0.42 | 0.39 | 0.61 | 0.72 | 0.67
Average Shear Stress N/mm2 | 0.41 |  |  | 0.67 |  | 
Increase in Shear Strength % | 63.4% |  |  |  |  | 

## Slide 21
BOND STRENGTH - NCAT
Maintains bond strength with lower residual bitumen content
Bond strength values consistently above 150 PSI
Bond strength
Specs: 100 PSI)

## Slide 22
Tack coat – MILLED SURFACE 100 % COATED

## Slide 23
PRIME COAT
Silane Water Solution
CSS1 + Silane Solution
Spraying
Treated Surface
Quick set 1 hour - no tire pickup
Waterproofed Surface

## Slide 24
SAFETY
Undulations Elimination ?
Sinking Bases Prevention ?
Bound stabilized layers with swell control and flexible bonding will reduce deflection values substantially
Reduced Fatigue of top layers

## Slide 25
Hill Roads – BETTER ROADS
STABILIZATION & WATERPRROFING OF SOILS |  | 
CRITICAL FACTOR | NANOTECHNOLOGY | BENEFITS
Waterproofed Base with low swelling & freeze – thaw | Swell reduction, Increase of MDD due to alkyl lubrication effect & nano inter-particle bonding | Waterproofed, stabilized flexible, low water permeability bases will eliminate undulation thereby improving safety

## Slide 26
Charge shielding and oil (alkyl) lubrication
Enables optimum compaction
Field proctor density of 100 to 105 have been observed
IMPROVED SOIL COMPACTION

## Slide 27
NANO BONDING WITH FLEXIBILITY, DURABILITY & IMPROVED STRENGTH
Cement Soil Stabilization
Silane + Nano Polymer + Cement
Proctor 95
Cementitious bonds degrade with time and lose strength due to wet and dry cycles - Low durability
Proctor 100 to 105
Unaffected by wet and dry cycles due to hydrophobicity - High durability
Cement Particle
ZycoBond Particle

## Slide 28
ORGANO SILANE TREATED SOIL DISPLAYED THE FOLLOWING,
Soil Swelling Reduced by 85 %
Compaction Density Increased by 4%
Sr | Parameters | Measure | Soil w/o additive | Soil + Cement 3% | Soil + Silane 0.75 kg/m3 + nano polymer 0.75 kg / m3 + Cement 3%
1 | CBR | % | 7 | 67 | 125
 |  | % Improvement | - | 857% | 1685%
2 | UCS | MPa | 0.27 | 1.02 | 2.43
 |  | % Improvement |  | 278% | 800%
3 | Durability (Wet – Dry Cycles) | No. of cycles | 0 | 4 | 12
 |  | IS : 4332 (Part 4) | Fails | Fails | Passes (Simulates 20 years life)
CRRI RESEARCH : EXECUTIVE SUMMARY

## Slide 29
Construction in Year 2010
Clayey Soil CBR 1.3 – 2.1, treated with Multi Layer Waterproofed Envelope
BHARTHALI - BHARTHNA ROAD, TAL. KARJAN, DIST. VADODARA, GUJARAT

## Slide 30
Post Monsoon Performance 2010 - 2013
BHARTHALI - BHARTHNA ROAD, TAL. KARJAN, DIST. VADODARA, GUJARAT

## Slide 31
Post Monsoon Performance 2014 - 2016
BHARTHALI - BHARTHNA ROAD, TAL. KARJAN, DIST. VADODARA, GUJARAT

## Slide 32
ESAL VALUE GAIN WITH WATER RESISTANCE
Description | IRC Design | IRC Design with Organo-Silane waterproofing (2.5% extra Cost) |  |  | 
Drainage Coefficient | 1 | 1.2 | 1.3 | 1.4 | 1.4 + 10% higher layer coefficient
Structural Number | 4.49 | 5.11 | 5.54 | 5.89 | 6.18
Equivalent MSA | 20 | 62 | 100 | 150 | 220
Times Improvement |  | 3 | 5 | 7.5 | 11

## Slide 33
THANK YOU