## Slide 1
Date : 18th August 2017 (Friday)
Location : CPWD HEADQUARTERS, New Delhi
ZYDEX NANOTECHNOLOGIES FOR BRIDGES REPAIR - AN OVERVIEW
Welcomes You

## Slide 2
Conserving Limiting Resources
through Innovation,
for a Sustainable world
Dr. AJAY RANKA
Zydex Industries Pvt. Ltd.

## Slide 3
REPAIR OF BRIDGES
Surface preparation
Bonding Technology
Construction Material
Protective Technology
Aesthetic Technology

## Slide 4
What are physiochemical processes at a bridge which destroy its physical structure & strength?
1) Wet & Dry Cycle (everyday on a water body or hills)
The Deterioration Process
Water penetrates into the most inaccessible micro cracks and nano capillaries, thus causing degeneration

## Slide 5
What are physiochemical processes at a bridge which destroys its physical structure & strength?
2) Carbonation
The Deterioration Process
CARBONATION REACTION
Calcium Hydroxide
Calcium Carbonate
H2O + CO2 ------------- H2CO3 (Carbonic Acid)
Ca(OH)2 + H2CO3 ------CaCO3 + 2H2O

## Slide 6
What are physiochemical processes at a bridge which destroys its physical structure & strength?
3) ASR (Alkali Silica Reaction)
The Deterioration Process
ALKALI-SILICA REACTION
Silicate
Silica Gel
Strong Base
[OH-]
=Si-O-Si= + H2O --------------- =Si-OH…….OH-Si=

## Slide 7
What are physiochemical processes at a bridge which destroys its physical structure & strength?
4) Corrosion
The Deterioration Process
ELECTROCHEMICAL CORROSION REACTIONS
Anode
Cathode
Fe++ + 2Cl-  FeCl2
FeCl2 + H2O + OH-  Fe(OH)2 + H+ + 2Cl-
2Fe(OH)2 + ½O2  Fe2O3 + 2H2O
½O2 + H2O + 2e-  2 OH-

## Slide 8
Current Problem: Cement Grade 53 – High initial strength & faster curing due to smaller particle size –But high surface area leads to formation of micro cracks
40 – 60 M grade concrete is used
Reduced porosity
Bridges - Material of Construction

## Slide 9
Repair Methodology – Surface Preparation
Mechanical cleaning: Clean the surface by chipping and removing all the loose concrete / mortar debris, dirt or fungal deposits. Remove laitance, if present in the peripheral zone.
Power tools can be used to achieve this.
Clean the dust by pneumatic air pressure with portable blowers.

## Slide 10: Nanotechnology in Bonding
Bonding Strength: Very High & Penetrative
A nano particle will have excellent wetting & bonding ability to all ferrous oxide, ferric oxide, metal, cement and sand particles. All micro & nano porosities gets mechanical impregnation. Imparts chemical bonding & flexibility.
Repair Methodology – Bonding Technology

## Slide 11: Particle size: 70 – 90 nm
Water Resistant
  See boil test
  See nail test
  See drop test
Nano range can penetrate into
M30 – 40 – 50 concrete also.
Nanotechnology in Bonding
Repair Methodology – Bonding Technology

## Slide 12
Test Results / Videos
≈ 34 kN
STRENGTH
  Concrete to Concrete
  Concrete to Plaster
  Plaster to Granite / Stone / Tiles
Repair Methodology – Bonding Technology
Heavy Granite with ColdBond
Plaster with ColdBond
ColdBond vs Tile Adhesives

## Slide 13
Pull-off adhesion strength registered – 34 kN (3467 kgs.)
That is, 17.32 N/mm²
PULL-OFF ADHESION RESULTS

## Slide 14
Plaster should be cement + Graded sand / Precipitated silica / Fumed silica + Polymer to impart high flexibility
Repair Methodology – Construction Material
Repair with PMM (Polymer Modified Mortar)

## Slide 15
Post 2 weeks of curing, waterproof with penetrative nanotechnology with a bonder in it.
Acts like anti-carbonation barrier.
All fine and micro pores will be sealed and surface is primed for painting.
Repair Methodology – Protective Technology
Does not leach out or wash out due to chemical bonding & penetration
Over 20+ years UV stability (tested as per ASTM G-154)
O
Si
Si
O
Zycosil
Zycosil
O
Si
Si
O
O
Si
Si
O
O
Si
Si
O
O
Si
Si
Organofunctional Long Chain Molecule Group
Nature’s
Strongest
Bond

## Slide 16
Concrete
Makes Surface
Water Resistant
Breathable surface
Allows Vapor
to Escape
UV & Heat Resistant
(Penetrative & Reactive)

## Slide 17
Apply a weather resistant 100% acrylic paint.
The paint should be breathable.
Zydex Silver Paint to be applied in 2 coats without primer.
Repair Methodology – Aesthetic Technology
Tested for:
Drying Time (surface dry / hard dry)
Finish
Colour
Washability & Cleanability
Temperature Stability
Resistance to Alkali
Zydex Silver Paint conforms to IS:15489-2004 Indian Standard for Plastic Paint Emulsions

## Slide 18
Cost | Activity
Rs.70 per m² | Spray Bonding with ColdBond
Up to Rs.200 / m² | Polymer Modified Plaster with Elastobar
Rs.80 / m² | Waterproofing with Zycosil+
Rs.50 / m² | Paint with Zydex Silver
+
Surface preparation cost, as per site conditions
+
Labour, Overheads and profit for Contractor
Indicative cost per m² basis for estimation

## Slide 19
Construction / Cold Joints Bonding
Technologies for New Construction
Protective surface treatment
Weather resistant painting